# dGray’s Furniture Restoration & Refinishing

#### Process of Refinishing

# Pick Up & Delivery

- Capability to deliver without damaging - (dings, dents, & scratches)

# Restoring & Refurbishing

- Dismantle removable parts and label

- Check for any splits or cracks in the grain of wood

- Manufacture/replace missing parts or pieces of wood

- Alternate options of using wood body filler to replace missing wood

- Reassemble

- Re glue

- Clamp and screw in place to ensure a tight clean fit

- Let glue cure

- Prepare to strip or clean

## Stripping and/or cleaning

- Prepare pieces to be stripped

- Score/mark individual pieces for final assembly- i.e. table leafs

- Strip in a pan by hand dipping – not total submersion

- Paying particular attention to corners, roundels, etc.

- Ensure finish is removed from the pores of the wood – when practical and possible

- Neutralize with #270 Industrial Paint Thinner

Or

- Clean with a 50/50 mix ammonia and water to remove accumulated dirt and polish

- Neutralize with clean water

- Let dry

## Sanding and Filling

- Steam with iron and cold wet cloth to raise the grains, dings and/or dents

- Changing the water frequently to help pull out the rest of any color in the wood

- Fill gouges, dents and dings, which are left, with wood body filler

- Sand:

-Determine to what degree by following Daily Production Log

-Utilize air sanders and/or electrical sanders to achieve a uniform sanding

-Sand with different degrees of grit in ascending order

(80,100,120,150,180,220,280,320,400,600)

-Sand with the grain until desired “smoothness” is reached

-Final hand sand with the next ascending degree of sandpaper to sand out

any sanding marks

- Blow off sanding sawdust with air hose

- Tack cloth to remove any residual particles

- Spray sealing lacquer on any exposed wood – including backs

(light misting coat , to seal wood grain but not the pores of the wood)

- Sand lightly with 280 grit to smooth sealer and prepare for filler

- “Paint” on filler- choosing appropriate filler by following Daily Production Log to achieve start of the customers desired color

- Let dry to a powdery consistency

- Sand filler to remove any excess and to achieve desired hue

- Blend any dark to light areas in the grains of the wood by sanding

### Finishing

- Choose the proper stain to start the coloring process to achieve customers color choice

- Stain with rag and China Bristol brush – clean brush properly

- Grain (color) wood body filler to match surrounding wood with graining pencils or china markers

- And/or spray penetrating stain blended with lacquer to match customers specifications

-While maintaining a blended effect to insure a consistent color for the

whole piece

# Sand lightly - if necessary

- 1st coat of lacquer – Gloss for clarity of existing wood color

- Sand to smooth – lightly

- 2nd coat of lacquer

-Add penetrating stain to match and blend colors of different grains in  wood

-Detail or highlight areas that need blending

-Utilizing Mohawk toner and/or Mohawk color spray cans

-Recoat with lacquer to seal color in

# Sand to a slick finish

-Using 280 grit sandpaper on an orbital air sander

-Resand by hand to remove any sanding “chatter” marks

-Avoid cutting through any edges or corners

- Detail corners & edges with touch up markers, china markers and/or edging sticks

- Finish any/all touch up areas with padding stains before 3rd coat of lacquer

- 3rd coat of lacquer

-Spray a quality, heavy, consistent coat

-sand as needed (to remove any orange peels or blemishes)

- Hand rub finish to produce a very slick finish in preparation of final coat

- Final coat

-Allow curing 1-3 days (depending on customers “sheen” request)

-To customer’s request – Sheen’s: Dull, Satin, Semi-gloss, Gloss, Rubbed, Polished, Buffed

- Call customer to set up delivery

### Finishing Touches

# Reinstall polished hardware

- Load furniture into delivery vehicle

-Pad with furniture pads –paying attention to corners, etc.

-Tie down with nylon and/or bungee cords-no rope burns

- Deliver

-While maintaining a “Successful Delivery” (a delivery free of error)