# dGray’s Furniture Restoration & Refinishing

#### Process of Resurfacing

Cleaning

- Clean with a 50/50 mix ammonia and water to remove accumulated dirt and polish

- Neutralize with clean water

- Let dry

## Sanding and Filling

- Fill gouges, dents and dings, which are left, with wood body filler

- Sand:

-Sand with the grain until desired “smoothness” is reached

### Finishing

# Use stain of existing wood color with rag

- 1st coat of lacquer

- Sand to smooth – lightly

- 2nd coat of lacquer

-Allow curing 1-3 days

### Finishing Touches

# Reinstall polished hardware